1.  Exteriorguard® guardrail components shall be designed in accordance with NBC, AISC and CSA

standards listed in §13145.3.

2.  Exteriorguard® post baseplates shall be made of (10” x 10” x ½”) material welded to HSS  (5” x 5”)

tubular  ASTM 500 Grade C metal.  Height of posts shall be 44” for double high rail.  Posts are pre-

punched  to accommodate ½” diameter fasteners.  Posts shall be designed to accommodate various

rail heights.

3.  Exteriorguard® shall have  12” high rails with welded side brackets that are manufactured with

ASTM  A607 Grade 50 corrugated steel.  Installed rail shall be 42” high for double post.

Rail lengths shall be 2 feet to 8 feet nominal.

4.  All components for Exteriorguard® series guardrail shall be powder coated one coat of highly visible

safety yellow paint and are intended for outdoor use.

5.  Exteriorguard® guardrail system shall incorporate a pass through post fastener design.

The (½” x 7”) galvanized carriage bolt shall pass completely through the post and rail bracket.

Bolt shall be secured with washer and nut.  Nut shall be tightened 1/3 turn past snug  tight condition.

Post plates shall be affixed to concrete floor by 4-1/2” x 5/8” galvanized wedge anchors in at least

6” of good concrete.

6.  The guardrail shall be installed at least 12” away from the surface to be protected.  This minimal

distance is necessary for deflection of an impacted rail.

7.  Total system shall be designed to meet or exceed a rating of 10,000 lb. at 4 mph breakthrough when

installed in proper concrete depth.

# Text boxes

NOMINAL LENGTH

12”